## Slide 1
Steel fragilization due to emergency depressurization real-scale experiment and modelling
Hazards 32 - Harrogate

## Slide 2: Summary
STEEL FRAGILISATION AFTER DEPRESSURISATION OPERATIONS
EXPERIMENTAL SET-UP
EXPERIMENTAL RESULTS
COMPARISON WITH SYMMETRY SIMULATIONS
CONCLUSION
01
02
03
04
05

## Slide 3
01 - STEEL FRAGILISATION AFTER DEPRESSURISATION OPERATIONS
Hazards 32

## Slide 4: GRTgaz in few words
Hydrogen to decarbonise energy sector
  A challenge for the gas industry to answer to climate change and rarefaction
  New strategies and roadmaps defined by national governments and the EU for the development of hydrogen technologies
A common goal for TSOs
  31 european energy infrastructure operators are creating the European Hydrogen Backbone (EHB)
  Roadmap up to 2040
  53,000 km based on using 60% of repurposed natural gas pipelines and 40% new pipelines
  Investments from 80 to 140 billions € (70 to 125 b£)
European Hydrogen Backbone (2022)

## Slide 5: GRTgaz: commitment to limit greenhouse gas emissions
Internal policy to reduce GHG emissions
  GRTaz defined a trajectory to follow COP 21 agreement objectives
  To achieve these objectives Methane emissions is a priority
    Methane is about 45% of scope 1 and scope 2 emissions in 2019
    Reinforcement of the use of gas booster technique (used since 2009): now 90% of gas is recovered
    Flaring of most of the other releases: GHG reduction factor of 25
  Energy consumption management is another key
    ISO 50001 certification for its energy performance and consumption
    ISO 14001 environment certification for all its compressor stations
  Fruitful effort to be continued
    2016 to 2019: -43% of GHG emissions
    2019 to 2021: -30.5 % of GHG emissions

## Slide 6: Emissions for emergency reasons
Depressurisation outside normal operations
  Two main scenarios
    Pressure exceedance on gas network
    Gas detection in compressor hall
  Outside GHG emissions a potential risk to study
    Local authorities ask about steel fragilization after these sudden depressurization
    From several tens of bars to ambient pressure
    Released gas cool down pipe walls
    GRTgaz must demonstrate that pipe wall temperature may not be lower than the limit allowed for steel integrity
    Aim : avoid a steel fragilization that could cause an uncontrolled gas release along the feed gas and vent lines

## Slide 7: Temperature criteria for steel pipe
Eurocode 3 standard
  Allowed temperature difference with temperature of assembly: +/- 35°C
  Temperature must be between -40°C and +60°C
Gas temperature during the depressurisation
  Rule of thumb : -0.5 °C per bar loss
  Temperature drop of -30 / -40°C is expected for gas at exit
  What about the steel temperature ? Along the line ? At vent stack ?
GRTgaz approach
  Experimental work: temperature measurement during an emergency depressurization
  Modeling work
    Validate the SYMMETRY software on experiment
    Simulate the other configurations

## Slide 8
02 - EXPERIMENTAL SET-UP
Hazards 32

## Slide 9: Experimental set-up
Test site: Etrez compressor station
  Location
    About 100km north from Lyon (Southwest of France)
    Close to an underground storage operated by Storengy (Engie Group), also located in Etrez
  Main characteristics
    Equipped with 3 electric-driven compressors
    Connects 8 pipelines (diameter from 450 to 120mm)
    Maximal operating pressures: 67.7 or 80bar (g.).

## Slide 10: Experimental set-up
Test site: Etrez compressor station
  Emergency depressurisation on Etrez 2
    Initial pressure: 49 bar
    Purged system: 600mm diameter pipe of 800m long + secondary lines (total length: 2070m)
    Vent line : 100mm diameter pipe of 300m long
Vent platform
Etrez 2

## Slide 11: Experimental set-up
Test site: Etrez compressor station
  Temperature measurements
    At vent stack: 4 temperature probes (PT100)
Temperature probes PT100-1 and PT100-2 (upper vent)
Temperature probes PT100-3 and PT100-4 (lower vent)
Silencer
Vent line
40mm
100mm
H = 1450 mm
H = 150 mm
H = 55 mm
400mm

## Slide 12: Experimental set-up
Test site: Etrez compressor station
  Temperature measurements
    Inside the Emergency Shut-down (ESD) pit
    Temperature probes used for process operations near compressors and air-cooling system are also recorded
  Other measurements
    Gas composition analyzed during the test period
    Pressure from process data system (SCADA)
Thermocouples TC1 and TC2
(ESD pit)

## Slide 13
03 - EXPERIMENTAL RESULTS
Hazards 32

## Slide 14: Experimental results
Main information
  The depressurization drops from 49 bar(g) to ambient pressure in about 30 min
  Minimal temperatures recorded by the thermal probes are between -6°C to 1.2 °C depending on the location.
  For an initial temperature between 10 to 15°C, the temperature drop is about -14 to -17°C
Probes | Initial temperature (°C) | Minimal temperature (°C) | Temperature drop (°C)
TIT35 (upstream compressor) | 15.1 | -1.6 | -16.6
TIT76 (downstream compressor) | 15.1 | 1.2 | -13.9
TIT74 (upstream aircooler) | 10.3 | -6.1 | -16.4
PT100-1 / PT100-2 (upper vent) | 7.9 / 7.8 | -7.3 / -8.5 | -15.2 / -16.3
PT100-3 / PT100-4 (lower vent) | 9.1 / 9.5 | 1 / 0.4 | -8.1 / -9.1
TC 1/ TC 2 (ESD pit) | 9.5 / 10.3 | -4.3 / -4.1 | -13.8 / -14.4

## Slide 15: Experimental results
Temperature measurements during the depressurization test (process probes)
Temperature measurement during the depressurization test (test probes)

## Slide 16
04 - COMPARISON WITH SYMMETRY SIMULATIONS
Hazards 32

## Slide 17: COMPARISON WITH SYMMETRY SIMULATIONS
SYMMETRY chosen for flow modeling
  Software developed by VMG (Schlumberger)
  Use for process calculations for sizing and flow assurance
  A dynamic mode to simulate vessel and/or networks depressurization by considering heat transfer and fluid dynamics
  SYMMETRY couples several 1D models for each phenomenon, with a large panel of options and submodels to adjust accuracy and computational time
Visuel SYMMETRY

## Slide 18: COMPARISON WITH SYMMETRY SIMULATIONS
Simulations set-up
  Real gas mixtures is implemented
  Thermodynamics properties calculated with Advanded Peng Robinson Natural Gas 2 (recommended by Schlumberger)
  Crane model (default) used to estimate the pressure drop for fittings and valves. Each part is characterized by its K-factor from an extensive database
  Colebrook model used to estimate the pressure drop due to friction along the pipeline
Gas compounds | Mole fraction
Methane | 0.949
Nitrogen | 0.0035
Carbon dioxide | 0.0024
Ethane | 0.039
Propane | 0.0042
Isobutane | 0.0009
n-Butane | 0.0006
Isopentane | 0.0002
n-Pentane | 0.0001
n-Hexane | 0.0001
With :
DP : pressure drop due to friction along the pipeline (Pa)
F : friction factor
L : pipe length (m)
D : pipe diameter (m)
r : gas density (kg/m3)
V : gas velocity (m/s)
e : pipeline roughness (m)  40 µm steel pipe with several years of operation
Re : Reynolds number

## Slide 19: COMPARISON WITH SYMMETRY SIMULATIONS
Simulations set-up
  Heat transfer between steel pipe and ambient air or ground
    For buried pipes: the “Ground-T based” model is used and recommended for fully buried pipe
    For buried pipes: the ground temperature set at 20°C, with a conduction constant of 1.5 W.m-1.K-1
    For above ground pipes: natural convection is calculated by considering a constant heat transfer coefficient and ambient temperature (10°C)
  Inner convection is calculated with the HTube mix model based on Dittus-Boelter correlations
  Several options in the dynamic solver to adjust accuracy of transient calculations
    For venting : the full Do Pipe Transient DP Calc model is selected to obtain more accurate results (developers’ recommendations)
  Difficulty to model the silencer at vent exit
    Interior of the silencer is neglected, even though it may affect pressure drop
    Pipe reduction of 40mm diameter creates a sudden change in the flow: numerical unstability after a relatively large simulation time.
40mm
100mm
400mm

## Slide 20: COMPARISON WITH SYMMETRY SIMULATIONS
Simulations results
  SYMMETRY perfectly estimates the pressure decrease

## Slide 21: COMPARISON WITH SYMMETRY SIMULATIONS
Simulations results
  Good prediction of the minimal temperature
    Deviation of less than 2°C
    Slope of temperature decrease is very similar with the experimental curve
    Numerical instabilities at upper vent due to pipe reduction in the silencer: smoother results in neglecting the reduction but less accurate results
Upper vent
Lower vent
ESD pit

## Slide 22
06 – CONCLUSION
Hazards 32

## Slide 23: Conclusion
  The experimental trials of Etrez give valuable data about the pipe temperature decrease during an emergency depressurization.
  The temperature drop is about -8 to -17 °C, under the tested conditions. These values enable to build an argument to justify the choice of steel grades and explain that no damage or unusual fatigue are expected after this kind of depressurization.
  The comparison of SYMMETRY with these data helps estimation of the accuracy of simulation to predict similar depressurization.
  The comparison indicates a very good agreement with pressure and temperature measurements.
  Consequently, with the validated setup, it is possible to simulate depressurization with different pipe geometries and different initial conditions to estimate the risk due to cold gas. Such simulations are ongoing for depressurization at sectioning stations.
  This work will help GRTgaz to answer to the local authorities

## Slide 24: Any questions ?